QwikSet™ Mirro-Mastic®

Directions for Substrate and Mirror Preparation - Do not use on acrylic mirror, vinyl safety backing, a painted surface, wall covering, or treated wood. - For best adhesion, the mirror, substrate, and mastic should be at room temperature (72ºF, 22ºC). - Make sure mirror and substrate are free of dust, clean and dry. On nonporous substrates, such as glass, tile, or metal, sealing is not necessary. On porous substrates, such as drywall or wood, use a primer or sealer (not paint or Mirro-Mastic Bond) and allow it to dry. Painted surfaces should be sanded through to the original surface and the substrate cleaned and sealed where the mastic is to be applied. Wall coverings should be removed and the substrate cleaned and sealed where the mastic is to be applied. - Support mirror at the bottom. Mechanical fasteners should be used for all mirror applications.

Directions for use of QwikSet™ Mirro-Mastic® Apply QwikSet™ to the mirror or substrate in vertical beads or mounds. Do not apply mastic too close to the edge, to prevent "squeeze out". Place the beads or mounds so space will be left between them when the mirror is installed. Each vertical bead should be approximately 1/2 inch (13 millimeters) in width with a minimum of one bead for every foot (305 millimeters) of mirror. Each mound of QwikSet™ should be approximately 1-1/2 inches (38 millimeters) in diameter with a minimum of one mound for every square foot (929 square centimeters) of mirror. - Press mirror firmly in place, making good contact between the mirror, mastic and substrate. Each vertical bead should spread to approximately 2 inches (51 millimeters) in width and each mound should spread to a pat approximately 3-1/2 inches (89 millimeters) in diameter. The mastic needs air circulation to cure properly. At room temperature, QwikSet™ will cure to approximately 80% strength in 48 hours. Curing time will depend on temperature, humidity, type of substrate, and amount of air that can reach the mastic. - With minimum coverage, one cartridge of QwikSet™ will install approximately 20 square feet (1.9 square meters) of mirror. - Clean-up can be done with mineral spirits. For ceiling applications or for technical questions not covered in our directions, please contact CRL Technical Sales (800) 421-6144, Ext. 777 or by e-mail at techsales@crlaurence.com.

WARRANTY DISCLAIMER

Nothing herein shall be deemed to constitute a warranty, either express or implied, by Palmer Products Corporation with respect to Mirro-Mastic®  or any other Palmer product. Palmer hereby disclaims all warranties, including without limitation, implied warranties of merchantability and fitness for a particular purpose. This disclaimer shall extend to all users of Palmer products and to any third party.  Any dispute or claim of whatsoever type arising out of the use of any Palmer product shall be governed by the laws of the Commonwealth of Kentucky. Palmer's sole liability, if any, and any user's or third party claimant's sole and exclusive remedy relating to any such dispute or claim shall be replacement of the Palmer product used.

Caution: Flammable

Vapors may ignite explosively; prevent buildup of vapors. Open all windows and doors. Use only with cross ventilation. Do not smoke. Keep away from heat, sparks and open flame. Close containers after use.

Use on 1/8 inch (3 millimeters) mirror and certain substrates may result in distortion.